Masking tape Specification (TDS)
	Properties(특징)
	Unit(단위)
	Acceptable
	CP088R

	Total thickness
	mm
	110÷150
	0.130 ±0.1mm

	Backing thickness
	
	75÷115
	0.95±0.1mm

	Adhesion to steel
	N/25mm
	2.5÷7.25
	4.8

	Adhesion to backing
	
	1.5÷5
	3.25

	Shear adhesion Met
(50℃;19)
	min
	>5
	15

	Tensile Strength
	N/25mm
	70÷112.5
	87.5

	RBT
	cm
	0÷3
	1

	Total weight
	g/m2
	93÷107
	100

	Backing weight
	
	56÷66
	61

	Adhesive weight
	
	37÷41
	39

	Elongation
	%
	Min,
	8

	Temp.resistance
to stainless steel
	℃
	Max.
	80

	
	Min
	
	30

	Waterproof property
	
	
	O

	Adhesive type
	
	
	Rubber solvent based

	Backing
	
	
	Saturated water proof

	Color
	
	
	Red



*주의사항
1. 직사광선을 피해서 보관하여 주시고, 23℃ 이상, 습도 50%이상 환경은 피해 주십시오.
2. 유통기한: 완제품인 경우 6개월 초과 하지 말아 주십시오.
