Masking tape Specification (TDS)

| Properties(특징) | Unit(단위) | Acceptable | CP088R |
| --- | --- | --- | --- |
| Total thickness | mm | 110÷150 | 0.130 ±0.1mm |
| Backing thickness |  | 75÷115 | 0.95±0.1mm |
| Adhesion to steel | N/25mm | 2.5÷7.25 | 4.8 |
| Adhesion to backing |  | 1.5÷5 | 3.25 |
| Shear adhesion Met (50℃;19) | min | >5 | 15 |
| Tensile Strength | N/25mm | 70÷112.5 | 87.5 |
| RBT | cm | 0÷3 | 1 |
| Total weight | g/m2 | 93÷107 | 100 |
| Backing weight |  | 56÷66 | 61 |
| Adhesive weight |  | 37÷41 | 39 |
| Elongation | % | Min, | 8 |
| Temp.resistance to stainless steel | ℃ | Max. | 80 |
|  | Min |  | 30 |
| Waterproof property |  |  | O |
| Adhesive type |  |  | Rubber solvent based |
| Backing |  |  | Saturated water proof |
| Color |  |  | Red |

*주의사항

1. 직사광선을 피해서 보관하여 주시고, 23℃ 이상, 습도 50%이상 환경은 피해 주십시오.

2. 유통기한: 완제품인 경우 6개월 초과 하지 말아 주십시오.