Masking tape Specification (TDS)

| Properties(특징) | Unit(단위) |  | CP094 |
| --- | --- | --- | --- |
| Total thickness | mm |  | 0.15 ±0.015mm |
| Steel Adhesion | g/inch | Min. | 500 |
|  | N/100mm |  | 19.3 |
|  | OZ/IN |  | 17.64 |
| Initial tack | mm | Max. | 20 |
| Holding power | Hours | Min | 30 |
| Tensile Strength | Kg/15mm | Min. | 4.6 |
|  | N/100mm |  | 300.74 |
|  | IB/IN |  | 17.17 |
| Elongation | % | Min, | 6 |
| Temp.resistance to stainless steel | ℃ | Max. | 95 |
|  | ℉ |  | 203 |
| Waterproof property |  |  | X |
| Adhesive type |  |  | Solvent based natural Rubber |
| Backing |  |  | Crepe paper |
| Color |  |  | Light yellow |

*주의사항

1. 직사광선을 피해서 보관하여 주시고, 23℃ 이상, 습도 50%이상 환경은 피해 주십시오.

2. 유통기한: 완제품인 경우 6개월 초과 하지 말아 주십시오.