Masking tape Specification (TDS)
	Properties(특징)
	Unit(단위)
	
	CP094

	Total thickness
	mm
	
	0.15 ±0.015mm

	Steel Adhesion
	g/inch
	Min.
	500

	
	N/100mm
	
	19.3

	
	OZ/IN
	
	17.64

	Initial tack
	mm
	Max.
	20

	Holding power
	Hours
	Min
	30

	Tensile Strength
	Kg/15mm
	Min.
	4.6

	
	N/100mm
	
	300.74

	
	IB/IN
	
	17.17

	Elongation
	%
	Min,
	6

	Temp.resistance
to stainless steel
	℃
	Max.
	95

	
	℉
	
	203

	Waterproof property
	
	
	X

	Adhesive type
	
	
	Solvent based natural Rubber

	Backing
	
	
	Crepe paper

	Color
	
	
	Light yellow




*주의사항
1. 직사광선을 피해서 보관하여 주시고, 23℃ 이상, 습도 50%이상 환경은 피해 주십시오.
2. 유통기한: 완제품인 경우 6개월 초과 하지 말아 주십시오.
