Masking tape Specification (TDS)

| Properties(특징) | Unit(단위) |  | CP100 |
| --- | --- | --- | --- |
| Total thickness | mm |  | 0.135 ±0.15mm |
| paper thickness |  |  | 0.11±0.15mm |
| Adhesion to steel | N/25mm |  | 5±1 |
| Tensile Strength | N/25mm |  | 110±20 |
| Total weight | g/m2 |  | 100±1 |
| Backing weight |  |  | 60±3 |
| Adhesive weight |  |  | 40±1 |
| Elongation | % | Min, | 10±2 |
| Temp.resistance to stainless steel | ℃ | Max. | 120 |
|  | Min |  | 30 |
| Waterproof property |  |  | O |
| Adhesive type |  |  | Solvented-based Natural Rubber |
| Backing |  |  | Impregnated Crepe paper |
| Color |  |  | Orange |

*주의사항

1. 직사광선을 피해서 보관하여 주시고, 23℃ 이상, 습도 50%이상 환경은 피해 주십시오.

2. 유통기한: 완제품인 경우 6개월 초과 하지 말아 주십시오.