Masking tape Specification (TDS)
	Properties(특징)
	Unit(단위)
	
	CP100

	Total thickness
	mm
	
	0.135 ±0.15mm

	paper thickness
	
	
	0.11±0.15mm

	Adhesion to steel
	N/25mm
	
	5±1

	Tensile Strength
	N/25mm
	
	110±20

	Total weight
	g/m2
	
	100±1

	Backing weight
	
	
	60±3

	Adhesive weight
	
	
	40±1

	Elongation
	%
	Min,
	10±2

	Temp.resistance
to stainless steel
	℃
	Max.
	120

	
	Min
	
	30

	Waterproof property
	
	
	O

	Adhesive type
	
	
	Solvented-based
Natural Rubber

	Backing
	
	
	Impregnated Crepe paper

	Color
	
	
	Orange




*주의사항
1. 직사광선을 피해서 보관하여 주시고, 23℃ 이상, 습도 50%이상 환경은 피해 주십시오.
2. 유통기한: 완제품인 경우 6개월 초과 하지 말아 주십시오.
